The present invention relates to the modification of polymeric materials and can be used for the preparation of electrical conductive sulphidic coatings on polymers thus enabling galvanic metallization thereof.
To obtain electrical conductive coating on low-density polyethylene film the latter is treated with 0,002 M polythionic acid, washed up with water and then treated with the solution of copper salt and hydroquinone.