The present invention relates to a method for a formation of the electrical conductive coatings on polymers. The electric conductive selenidic coatings  are prepared by selenidic coating the polycaproamidic films in 0,05-0,1 M acidic solution of potassium selenothrithionate, washing with water and treating with the copper salt solution.@The polymeric materials modificated by this method show improved properties and can be used in galvanic metallization.