The present invention relates to the process for preparing amber adornments. The new feature of the process consisting of preparing raw amber, heating and compressing thereof, are that the raw amber is subjected to polishing for 120-180 minutes; washed with water; dried; soaked for 70-80 minutes in the solution consisting of 20 % of alcohol (not less than of 93 degrees), 20 % of butylacetate or ethylacetate, 60 % of toluene; dried again; then the amber-coat is removed, the small particles removed by sieving and the amber washed for 5-10 minutes with the solution mentioned aboved, dried, washed with water, dried again, sorted by colour and particles size, then poured into the press-form and heated in an owen for 70-90 °C at the temperature less than 240 °C; the press-form is then for 3-5 minutes subjected to pressure higher than 6.5 t/cm², heated for 20-30 minutes at temperature less than 240 °C and remained to cool down.