The present invention relates to a new photosensitive composition developable by an aqueous base solutions consisting of (in mass parts): a finely divided powder of inorganic filling material (100,0), a polymer (9-36), a photoinitiator (0,5-3,5), an organic disulfide (0,2-2,0), an inhibitor of thermopolymerization (0,01-0,35) and an organic solvent (5,5-21,5). This composition is useful in microelecronic application and has a low sensitivity to visible light and inhibits influence of oxygen.