The present invention relates to antimicrobial acetate threads. 5-Chloro-2-(2,4-dichlorophenoxy)-phenol as the additive to spinning solution is used. The threads composition is as follows:
acetylcellulose	-				86,9-89,4
antimicrobial additive -		 0,3- 2,5
oiling material -				 2,7- 3,3
acetone -						 0,3- 0,7
water -   						to 100.
Threads are active against various microorganisms, espacially against suppurative infections and can be used in medicine and textile.