The present invention relates to enterosorbents of ecologically harmful substances the enterosorbents being important human food supplements, and in particular to enterosorbents on the basis of natural minerals zeolite and shungite.@According to the invention claimed enterosorbent ZFCS is prepared from zeolite and shungite rock containing carbon in concentration of 27-32  %, enriching shungite with carbon up to carbon content 33±1 % , then providing magnetic separation to collect particles having diameter less than 1 µm and to put them into gelatine capsules. The latter are used orally in dose of 0,01 g per 1 kg of body weight with water purified with the same sorbent. At the initial moment of milling shungite with carbon content 33±1 % natural zeolite is added in ratio 1:1 and the process follows as a continuous cycle.