The present invention relates to the fibrous plant panels, specifically to the panels of hemp fibre that can be used in the manufacture of environmentally friendly furniture. Invention aims to produce a completely ecologically clean fibrous panel, without chemical additives, but with a good mechanical properties. The task is realized in that the mass, consisting of main components: hemp fibers and soft bast particles - 90-95 %, paraffin emulsion - 0,2-0,5 % and 5-6 % water, is chopped, swelled, diluted and from the mass are shaped panels. Chopped hemp fibers and soft bast particles are fed into the swelling chamber where the mass is swollen for 3-5 minutes at 180-200 oC and 10-12 atm, once again is crushed, diluted with circulation water 1.4 to 2 % concentration, is mixed with the paraffin emulsion, from the formed layer is collected water and the mass is hot-pressed at 90-220 oC.