The facade plate and its manufacturing method relate to construction industry, specifically the decorative finishing of the building's exterior walls. The composite layers of the facade panel consist  of three layers: gelket (1) mixed with hardener in a ratio of 50: 1, polyester resin (2), mixed with a hardener in a ratio of 50: 1, and a glass fiber emulsion membrane (3). The facade of the building can be of a variety of configurations and patterns. The production method includes a gradual filling of special shapes, with the desired writing and configuration, with composite layers. Spray / application gel (1) mixed with a hardener in a ratio of 50: 1, a layer of polyester resin (2) is applied to it, mixed with a hardener in a ratio of 50: 1, on which a layer of glass fiber emulsion mat (3)  is applied, all is set to roll and dry.