The invention relates to the field of electronics associated with the design and manufacture of semiconductor devices which require low contact resistance between titanium dioxide (TiO2) and p-type conductivity semiconductor. The proposed device is a layered structure comprised of a heavily doped p-type semiconductor layer and a n-type TiO2 layer arranged thereon, wherein a tunnel junction is formed between the said layers. In order to reduce the number of technological operations, time and materials by forming a low resistivity contact, the TiO2 layer is directly by atomic layer deposition (ALD) method deposited on the p- type semiconductor, wherein the part of the TiO2 layer adjacent to the said p-type semiconductor surface is additionally doped with niobium (Nb) donor impurity during the ALD-growth process, thus forming a tunnel junction between the TiO2 n-type layer and the p-type semiconductor.