The invention belongs to the field of construction industry, more precisely to cement concrete mixtures, which are subject to increased strength and durability requirements. The object of the invention is to provide a cement concrete mixture for the installation of a wear layer on the pavement of heavy traffic dominance zones, which has good mechanical and operational properties. Cement concrete mix containing a mixture of aggregates from fractionated chippings and sand, microsilica, cement, water, plasticizer, aggregate admixture and polypropylene fiber, characterized in that the aggregate mix consists of a 4-16 mm granite chippings fraction and a 0-4 mm sand fraction , the ratio of components by weight is: 4-16 mm granite chippings fraction 42.0-46.0; 0-4 mm sand fraction 31.6-34.9; microsilica 1.0-1.1; cement 14.2-15.5; plasticizer 0.07-0.08; pore forming additive 0.01-0.03; polypropylene fiber 0.40-0.44; water 5.7-6.3.