Method for the production of an organic mineral phosphogypsum aggregate consisting mainly of hemihydrate and calcium sulphate

Organic mineral filler can be used in the industry of various types construction materials, dry putties, technical rubber, artificial leather, paints, polymers and other products. This organic mineral filler consists of calcium sulphate hemihydrate, mainly. It is produced by heating phosphogypsum at a temperature of 550-600 C for 20-30 minutes.