The invention belongs to the field of construction industry and can be used for the installation of various structures, more precisely for railway and road acoustic barriers, their panels and their methods of manufacturing. The objects of the invention are to reduce and speed up the installation of acoustic barrier panels and also to improve the sound insulation. This railway and road acoustic barrier panel is comprised of a sound-insulating layer (1) which is made of rubber pellets from the used tyres 0,1 to 8 mm in size, adhesives as binders, additives such as odor control agents and flame retardants where 80-90 % by weight are the ruber pellets and 7-10 % are binders and the bonding plates (2).