The invention belongs to the field of the construction industry and can be used for partitions of various buildings, more precisely for inter-apartment partitions, where increased sound insulation requirements are imposed. The purpose of the invention is to create an inexpensive, thin inter-apartment partition with low load, good mechanical and operational properties, reduced cost of construction works and increased productivity of construction works by ensuring good sound retention and required noise standards. An inter-apartment partition, including at least one vertical sound-insulating panel (2) made of ground used tire pellets, plasterboard panels (1) at the edges of the partition, as well as fixing means (3) and a spacer (4) at the lower and upper base of the partition, where the inter-apartments the thickness of the partition is 100-140 mm, the thickness of the vertical sound insulating panels (2, 2') taken together is 45-70% of the thickness of the inter-apartment partition, and the means of fastening are the profile (3).