Composite finishing tile, its production method and use for ventilated building for the facade. For this finishing tile, a stone mass tile (1) with a thickness of 10 mm, polyurethane glue (2) is used for gluing, when the optimal layer of wet glue -the maximum permissible, due to the permissible heat capacity, is 0.140 mm, this polyurethane adhesive (2) is intended for to glue together various building materials, including metal with stone mass tile (1), where in this case a stainless steel sheet (3) with a thickness of 0.5 mm and an area corresponding to stone mass tiles (1) surface area,. The strong adhesion force after curing is 25 kg/cm2, extremely elastic seam - stretch to tear 450%. This composite tile meets the resistance impact category I, flammability class A2, due to smoke generation s2; due to flaming droplets or of particles d0.