The invention belongs to the field of construction industry. The purpose of the invention is to create good, diverse and bad aggregates for soils and unbound aggregate mixtures used to install railway, road and street embankments, bedrock and base layers, to improve and strengthen the applied additive that ensures the bearing capacity of the layer and resistance to environmental influences in all seasons. An additive is used for the improvement and strengthening of soils and unbound mixtures of several subgrade and base layers, which ensures the load-bearing capacity of the treated layer and resistance to environmental effects in all seasons, and differs in that the weight of the components of the additive in % of the total weight of the additive is: sulfuric acid - from 60 to 85; phosphoric acid - from 5 to 45; citric acid - from 5 to 45; at least one acidic surfactant - from 2 to 15; at least one trivalent metal compound - from 5 to 15; at least one aromatic hydrocarbon, especially β-naphthol - from 2 to 10. The additive is applied to primers and unbound aggregate mixtures in which the amount of particles smaller than 0.063 mm is 3-20%.